## Slide 1
Materials Science in Fusion Devices
Angela M. Capece
Department of Physics
The College of New Jersey
SULI Introductory Course
in Plasma Physics, PPPL
June 10, 2016

## Slide 2
A.M. Capece
Nuclear energy (fission & fusion) comes from the mass defect of the nucleus
Advantages of fusion energy:
Clean
Green
Safe
Abundant
MASS DEFECT:
The whole < the sum of the parts!
(e.g., mass of He nucleus is less than mass of 2p + 2n)
Larger mass defect  greater BE
Going from low BE to higher binding energy releases energy
2/51
SULI Introductory Course, 6/10/16
Notes: Hydrogen fuel extracted from seawater
D-D fusion can power the world for 2 billion years
  Coal – 200 yr
  Natural gas – 20 yr
  U235/Th232 breeder reactors – 20,000 yr
Fuel efficient
  City of 1 million, need 60 kg of H2

## Slide 3
A.M. Capece
We need fusion to survive
Advantages of fusion energy:
Clean
Green
Safe
Abundant
H fuel extracted from seawater
D-D fusion can power the world for 2x109 yr
  Coal: 200 yr
  Natural gas: 20 yr
  U235/Th232 breeder reactors: 20,000 yr
Fuel efficient
  City of 1 million, need 60 kg of H2
3/51
SULI Introductory Course, 6/10/16
Notes: Hydrogen fuel extracted from seawater
D-D fusion can power the world for 2 billion years
  Coal – 200 yr
  Natural gas – 20 yr
  U235/Th232 breeder reactors – 20,000 yr
  U – 200 yrs
Fuel efficient
  City of 1 million, need 60 kg of H2

## Slide 4
A.M. Capece
Hydrogen fusion requires high temperature & pressure  Plasma!
Temperatures of 100 million K are required (and have been achieved!)
The sun uses gravity to confine the plasma
We use magnetic fields
Magnets
Plasma
Is it possible on Earth?
YES! We’ve done it before. In fact, we did it here.
(Nov 2, 1994 – 10 megawatts of fusion power)
4/51
SULI Introductory Course, 6/10/16
Notes: Hydrogen fuel extracted from seawater
D-D fusion can power the world for 2 billion years
  Coal – 200 yr
  Natural gas – 20 yr
  U235/Th232 breeder reactors – 20,000 yr
Fuel efficient
  City of 1 million, need 60 kg of H2

## Slide 5
A.M. Capece
Hydrogen fusion requires high temperature & pressure  Plasma!
Magnets
Plasma
So why don’t we have it yet?
The trouble with fusion is…
  Confining enough hydrogen
  For long enough times
  At sufficiently high temperatures
5/51
SULI Introductory Course, 6/10/16
Notes: Hydrogen fuel extracted from seawater
D-D fusion can power the world for 2 billion years
  Coal – 200 yr
  Natural gas – 20 yr
  U235/Th232 breeder reactors – 20,000 yr
Fuel efficient
  City of 1 million, need 60 kg of H2

## Slide 6
A.M. Capece
Hydrogen fusion requires high temperature & pressure  Plasma!
Magnets
Plasma
So why don’t we have it yet?
The trouble with fusion is…
  Confining enough hydrogen
  For long enough times
  At sufficiently high temperatures
Better magnets
Better materials
We need…
6/51
SULI Introductory Course, 6/10/16
Notes: Hydrogen fuel extracted from seawater
D-D fusion can power the world for 2 billion years
  Coal – 200 yr
  Natural gas – 20 yr
  U235/Th232 breeder reactors – 20,000 yr
Fuel efficient
  City of 1 million, need 60 kg of H2

## Slide 7
A.M. Capece
Hydrogen fusion requires high temperature & pressure  Plasma!
Magnets
Plasma
So why don’t we have it yet?
The trouble with fusion is…
  Confining enough hydrogen
  For long enough times
  At sufficiently high temperatures
Better magnets
Better materials
We need…
7/51
SULI Introductory Course, 6/10/16
Notes: Hydrogen fuel extracted from seawater
D-D fusion can power the world for 2 billion years
  Coal – 200 yr
  Natural gas – 20 yr
  U235/Th232 breeder reactors – 20,000 yr
Fuel efficient
  City of 1 million, need 60 kg of H2

## Slide 8
A.M. Capece
What happens when you try to contain a plasma?
The plasma affects the surface
The surface affects the plasma
Plasma
Wall Material
  Physical & chemical properties of the material can change
Plasma
Wall Material
  Chemical composition of the plasma can change
8/51
SULI Introductory Course, 6/10/16

## Slide 9
A.M. Capece
Plasma
Wall Material
What do we have in the plasma?
How plasma affects the surface:
9/51
SULI Introductory Course, 6/10/16

## Slide 10
A.M. Capece
Plasma
Wall Material
What do we have in the plasma?
  High energy electrons
  H2, H, H2+, H+, He, He+
  neutrons
We have high energy particles & reactive species
How plasma affects the surface:
10/51
SULI Introductory Course, 6/10/16

## Slide 11
A.M. Capece
Plasma
Wall Material
What do we have in the plasma?
  High energy electrons, H2, H, H2+, H+, He, He+, neutrons
What do these species do?
  Impart energy to the wall (heating): ave loads are 10 MW/m2
  Erode the wall material
  Implant themselves in the wall – Limit on tritium retention!
  Do chemistry on the wall – form different compounds
  Can weaken the material – material swelling / embrittlement from neutrons, fuzz formation
How plasma affects the surface:
SULI Introductory Course, 6/10/16
11/51

## Slide 12
A.M. Capece
What do we have at the surface?
  A thermal sink (results in temperature gradients near the wall)
How the surface affects the plasma:
Plasma
Wall Material
Plasma
Material
108
106
104
102
Temperature (K)
Distance from the surface (m)
SULI Introductory Course, 6/10/16
12/51

## Slide 13
A.M. Capece
What else do we have at the surface?
  A thermal sink (results in temperature gradients near the wall)
  A nearly infinite source of impurities
  A source of electrons (from the atoms in the surface)
How the surface affects the plasma:
Plasma
Wall Material
SULI Introductory Course, 6/10/16
13/51

## Slide 14
A.M. Capece
What do we have at the surface?
  A thermal sink (results in temperature gradients near the wall)
  A nearly infinite source of impurities
    Impurities enter at low temps  reduction in plasma temperature!
    Dilute the fuel  leads to reduction in fusion power!
    Material deposited where it is not wanted (e.g., on an expensive diagnostic)
How the surface affects the plasma:
Plasma
Wall Material
SULI Introductory Course, 6/10/16
14/51

## Slide 15
A.M. Capece
What do we have at the surface?
  A thermal sink (results in temperature gradients near the wall)
  A nearly infinite source of impurities
  A source of electrons (from the atoms in the surface)
    Electron emission from the wall: cools the edge plasma & changes electric potential
    Results in gradients in temperature and potential  drives instabilities & reduced confinement
How the surface affects the plasma:
Plasma
Wall Material
SULI Introductory Course, 6/10/16
15/51

## Slide 16
A.M. Capece
Plasmas can be spectacularly destructive!
Melted tungsten tile
B. Lipschultz, Nucl. Fusion (2012)
Erosion of molybdenum
ion thruster grid
R.E. Wirz, IEEE Trans. Plasma Sci. (2008)
Tungsten tile in fusion device, before & after plasma exposure Z. Hartwig, MIT
Tungsten fuzz
M.J. Baldwin & R.P. Doerner, Nucl. Fusion (2008)
SULI Introductory Course, 6/10/16
16/51

## Slide 17
A.M. Capece
Five main processes that occur at the plasma-materials interface
SULI Introductory Course, 6/10/16
17/51

## Slide 18
A.M. Capece
Five main processes that occur at the plasma-materials interface
Positive Ion Neutralization (Recombination)
M.A. Lieberman, Principles of Plasma Discharges & Materials Processing
Occurs for all energies (10-1000 eV, typical)
All ions immediately neutralized
2 options:
-Electron enters excited state (radiates a photon as it transitions to lower state)
-Electron enters ground state & 2nd electron absorbs excess energy – Auger Neutralization also secondary electron emission (SEE)
SULI Introductory Course, 6/10/16
18/51

## Slide 19
A.M. Capece
Five main processes that occur at the plasma-materials interface
Positive Ion Neutralization (Recombination)
Bruining, Physica 5 (1938) 17.
SEE depends on the ion species and the composition of the solid
SEE yield of Be
SULI Introductory Course, 6/10/16
19/51

## Slide 20
A.M. Capece
Five main processes that occur at the plasma-materials interface
2. Absorption/Desorption (low energy, 1 eV)
Desorption of 1st order (a) & second order process (b)
http://users-phys.au.dk/philip/pictures/physicsfigures/node18.html
Rate equation for desorption:
(dependent on binding energy & temperature)
SULI Introductory Course, 6/10/16
20/51

## Slide 21
A.M. Capece
Five main processes that occur at the plasma-materials interface
3. Physical Sputtering (10-100 eV)
Sputtering
Higher energy transfer when masses are similar:
Rate equation:
Yield (empirical) = number sputters per incident ion
SULI Introductory Course, 6/10/16
21/51

## Slide 22
A.M. Capece
Five main processes that occur at the plasma-materials interface
3. Physical Sputtering (10-100 eV)
Sputtering
Sputter yields of silicon as a function of ion energy for noble gas ions:
http://xpssimplified.com/depth_profiling.php
SULI Introductory Course, 6/10/16
22/51

## Slide 23
A.M. Capece
Five main processes that occur at the plasma-materials interface
4. Implantation (1000 eV)
Implantation
http://www.abc.net.au/science/articles/2015/05/25/4229949.htm
5. Reactions with/on a surface
SULI Introductory Course, 6/10/16
23/51

## Slide 24
A.M. Capece
Five main processes that occur at the plasma-materials interface
Positive Ion Neutralization (Recombination)
Ions that hit the surface are neutralized
e + A+ + S A + S
Absorption/Desorption (low energy, 1 eV)
  Evaporation rate increases exponentially with temperature
Physical Sputtering (10-100 eV)
  Independent of surface temperature
Implantation (1000 eV)
Reactions with/on a surface
  Dependent on surface temperature
Sputtering
Implantation
Absorption/Desorption
SULI Introductory Course, 6/10/16
24/51

## Slide 25
A.M. Capece
Reality is much more complex!
Image from D. Whyte, http://psisc.org/mission
25/51
SULI Introductory Course, 6/10/16

## Slide 26
A.M. Capece
Some candidate materials and their properties
Graphite:
Does not melt (sublimes)
Erosion and transport occurs easily leading to C deposits
Can trap large amounts of tritium
Beryllium:
Low Z material
Good thermal conductivity
High sputter yields
Low melting point
Tungsten:
High Z material
Low sputter yield
High melting point
High Z materials (e.g. W, Mo):
Poison the plasma
Moderate uptake of tritium
Good thermo-mechanical properties
Low or negligible erosion at low plasma temperatures
SULI Introductory Course, 6/10/16
26/51

## Slide 27
A.M. Capece
Liquid metals
Advantages of liquid metals (lithium):
No erosion
No thermal fatigue
No neutron damage
Resilient again high heat fluxes
Refreshes the surface
Li concentration in the plasma is low
Infrared image of liquid lithium a fusion device at PPPL.
Flowing liquid Li experiment at University of Illinois at Urbana-Champaign
Li has shown to improve the plasma performance!
Improved confinement time  Very important for fusion!
SULI Introductory Course, 6/10/16
27/51
Notes: H will be re-emitted at low temp
Find material that will resist damage, while not allowing H to go back to the plasma
Flowing liquid Li!
Li improves plasma performance by absorbing all the H
Our experiments show that we can keep D in the walls until 700 K, so as long as we can control the walls to be at this temperature, we should be good!
Conclusions…. Plasma materials does two things
Renumber the pages
Check titles!
Save talk to jump drive

## Slide 28
A.M. Capece
But why does Li help?
High D retention  Low recycling  High edge temperature  Reduced temperature gradients
Recycling Process:
Through volumetric conversion of Li to LiD (Baldwin & Doerner)
2. Through complexes that involve oxygen (Krstic, Allain, Taylor)
Li absorbs D+ ions and “retains” them better than other materials
But how is D retained in Li?
Working hypothesis: Deuterium retention
SULI Introductory Course, 6/10/16
28/51
Notes: H will be re-emitted at low temp
Find material that will resist damage, while not allowing H to go back to the plasma
Flowing liquid Li!
Li improves plasma performance by absorbing all the H
Our experiments show that we can keep D in the walls until 700 K, so as long as we can control the walls to be at this temperature, we should be good!
Conclusions…. Plasma materials does two things
Renumber the pages
Check titles!
Save talk to jump drive

## Slide 29
A.M. Capece
Which material is best? We need to understand what happens at the surface!
Atoms at the surface behave differently than atoms in the bulk material.
The surface provides an environment where unique chemistry can occur.
So, how do we study surfaces?
Surfaces contain ~1014 atoms/cm2
Challenge: Detect 1014 cm-2 signal on a 1023 cm-3 background
SULI Introductory Course, 6/10/16
29/51

## Slide 30
A.M. Capece
Which material is best? We need to understand what happens at the surface!
Atoms at the surface behave differently than atoms in the bulk material.
The surface provides an environment where unique chemistry can occur.
So, how do we study surfaces?
Surfaces contain ~1014 atoms/cm2
Challenge: Detect 1014 cm-2 signal on a 1023 cm-3 background.
Solution: Use probes that strongly interact with matter, such as as electrons, ions, and photons (X-rays, UV light).
SULI Introductory Course, 6/10/16
30/51

## Slide 31
A.M. Capece
From the simple to the complex
Single crystal
Simple Model Experiments
More Complex Systems
Monoenergetic ion beam
(Image of He ions on phosphor screen)
TZM (Engineering materials)
Plasma sources / fusion devices
Grain boundaries
Alloying elements: Ti, Zr, C
Surface roughness
Multiple species, increased fluxes, atoms/ions/electrons/radicals
H+
H2+
H3+
SULI Introductory Course, 6/10/16
31/51

## Slide 32
A.M. Capece
From the simple to the complex
Simple Model Experiments
More Complex Systems
Laboratory surface science experiments
Linear plasma devices
Fusion devices
SULI Introductory Course, 6/10/16
32/51

## Slide 33
A.M. Capece
Laboratory surface science experiments
Test stand instrumentation in the
Surface Science & Technology Lab
Key variables affecting chemistry at surface:
  Pressure
  Temperature
  Composition
Lab-based surface science experiments enable independent control of all variables
  …something we cannot achieve in a tokamak or linear plasma device!
Isolate effects of:
  Chemistry
  Incident particle fluxes and energies
  Substrate temperature
  Surface composition
  Morphology
simple
complex
SULI Introductory Course, 6/10/16
33/51

## Slide 34
A.M. Capece
Laboratory surface science experiments
Test stand instrumentation in the
Surface Science & Technology Lab
simple
complex
Li
Li
SULI Introductory Course, 6/10/16
34/51

## Slide 35: Atomic-Level Diagnostics
 | Technique | Info Obtained | Additional Notes
 | X-ray Photoelectron Spectroscopy (XPS) / Auger Electron Spectroscopy (AES) | Chemical composition Oxidation state | Cannot detect H/D or He Probe depth ~10 nm
 | Temperature Programmed Desorption (TPD) | Desorption energy Rate constants | Detects H Can determine the total amount of an adsorbed species on the surface
 | Scanning Auger Microscopy (SAM) | 2D elemental map of surface Ion etching SEM images | Cannot detect H/D or He Can use ion etching to probe into deeper layers
 | Ion Scattering Spectroscopy (ISS) | Atoms/molecules in top 1-3 layers | Can use direct recoil spectroscopy to detect H/D
SULI Introductory Course, 6/10/16
35/51

## Slide 36
A.M. Capece
X-ray Photoelectron Spectroscopy (XPS)
Gives composition of top 5-10 nm
http://jacobs.physik.uni-saarland.de/english/instrumentation/uhvl.htm
SULI Introductory Course, 6/10/16
36/51

## Slide 37
A.M. Capece
Auger Electron Spectroscopy
37/51
SULI Introductory Course, 6/10/16

## Slide 38
A.M. Capece
Low-energy Ion Scattering Spectroscopy (LEISS)
Very surface sensitive
(probes top 1-3 layers)
He usually used for incident ion
38/51
SULI Introductory Course, 6/10/16

## Slide 39
A.M. Capece
Low-energy Ion Scattering Spectroscopy (LEISS)
Very surface sensitive
(probes top 1-3 layers)
He usually used for incident ion
39/51
SULI Introductory Course, 6/10/16

## Slide 40
A.M. Capece
Temperature programmed desorption
Sample
1 cm
Temperature Programmed Desorption (TPD) Technique:
Linear temperature ramp applied to sample
Partial pressure of desorbing species measured
Temperature of desorption peak relates to binding energy
Area under pressure vs. time curve proportional to number of atoms desorbed
40/51
SULI Introductory Course, 6/10/16
Notes: H will be re-emitted at low temp
Find material that will resist damage, while not allowing H to go back to the plasma
Flowing liquid Li!
Li improves plasma performance by absorbing all the H
Our experiments show that we can keep D in the walls until 700 K, so as long as we can control the walls to be at this temperature, we should be good!
Conclusions…. Plasma materials does two things
Renumber the pages
Check titles!
Save talk to jump drive

## Slide 41
A.M. Capece
Temperature programmed desorption
Sample
1 cm
Area under pressure vs. time curve  # of atoms desorbed
TPD can be used to measure D retention!
41/51
SULI Introductory Course, 6/10/16
Notes: H will be re-emitted at low temp
Find material that will resist damage, while not allowing H to go back to the plasma
Flowing liquid Li!
Li improves plasma performance by absorbing all the H
Our experiments show that we can keep D in the walls until 700 K, so as long as we can control the walls to be at this temperature, we should be good!
Conclusions…. Plasma materials does two things
Renumber the pages
Check titles!
Save talk to jump drive

## Slide 42
A.M. Capece
C.H. Skinner et al., JNM 438, S647 (2013)
Submonolayer Li Film
Submonolayer Li film on TZM stable up to 1000 K
Represents Li-Mo bonding
Desorption energy ~2.7 eV
Example: Desorption of Li from Mo
simple
complex
SULI Introductory Course, 6/10/16
42/51

## Slide 43
A.M. Capece
C.H. Skinner et al., JNM 438, S647 (2013)
Area under Li TPD curve increases with Li dose
Dipole interactions lower the desorption energy (~2 eV)
Ed is a function of coverage
Monolayer
Submonolayer
Example: Desorption of Li from Mo
simple
complex
43/51
SULI Introductory Course, 6/10/16

## Slide 44
A.M. Capece
Example: Desorption of Li from Mo
C.H. Skinner et al., JNM 438, S647 (2013)
Thick Li films (multilayer) evaporate at 500 K
Multilayer film represents Li-Li bonding
Cohesive energy of metallic Li ~1.7 eV
Complete
Monolayer
Submonolayer
Multilayer
simple
complex
SULI Introductory Course, 6/10/16
44/51

## Slide 45
A.M. Capece
TPD can be used to determine D retention
A.M. Capece, et al., JNM (2015)
In lithium films as function of temperature:
simple
complex
SULI Introductory Course, 6/10/16
45/51

## Slide 46
A.M. Capece
Lipschultz et al., (2010) MIT Report PSFC/RR-10-4
TPD can be used to determine D retention
In tungsten as function of fluence:
simple
complex
46/51
SULI Introductory Course, 6/10/16

## Slide 47
A.M. Capece
SEM used to understand fuzz & bubble formation in W
Tungsten fuzz
M.J. Baldwin & R.P. Doerner, Nucl. Fusion (2008)
S. Kajita, Nucl. Fusion 49 (2009) 095005
simple
complex
47/51
SULI Introductory Course, 6/10/16

## Slide 48
A.M. Capece
SEM used to understand fuzz & bubble formation in W
S. Kajita, Nucl. Fusion 49 (2009) 095005
simple
complex
48/51
SULI Introductory Course, 6/10/16

## Slide 49
A.M. Capece
Materials Analysis Particle Probe (MAPP)
Provides in-vacuo analysis of surface exposed to fusion plasma
Correlates plasma performance with the surface state
Provides immediate analysis
XPS: Elemental/chemical composition
Ion Scattering Spectroscopy:
IDs surface species
TPD: Gives binding energies, desorption products
Direct Recoil Spectroscopy: Can detect H
Courtesy of F. Bedoya
simple
complex
49/51
SULI Introductory Course, 6/10/16

## Slide 50
A.M. Capece
Materials Analysis Particle Probe (MAPP)
50/51
SULI Introductory Course, 6/10/16

## Slide 51
A.M. Capece
Key takeaway messages
The plasma and material are strongly coupled!
Key PMI issues in fusion devices include: heat loading, erosion, fuel dilution, tritium retention, nuclear embrittlement
So far, no perfect fusion material exists. Candidates are graphite, tungsten, beryllium, lithium
Surface science can help to understand and diagnose the surface in model experiments that can help simulate the tokamak environment
A variety of experiments of differing complexity are needed
51/51
SULI Introductory Course, 6/10/16