## Slide 1: Tritium Breeding Blankets for Nuclear Fusion Reactors
Monica Gehrig, PhD
Paul Humrickhouse, PhD
Blanket and Fuel Cycle Group
Fusion Energy Division

## Slide 2: A lot goes into making fusion work

## Slide 3: Fusion produces high energy neutrons
D+T  He (3.5 MeV) + n (14.1 MeV)
How can we use those neutrons?
What challenges do those neutrons present?

## Slide 4: The need for tritium breeding
The D-T fusion reaction is most attainable
Tritium has a (relatively) short half-life
Small amounts produced by fission reactors
Need tritium supply, with a tritium breeding ratio (TBR) > 1*
Notes: The D-T fusion reaction is most attainable
Tritium decays with a 12.3 year half-life, decays into helium
Small amounts produced by fission reactors can supply short-pulse research devices
- For some context, a fusion reactor will require 55.6 kg of tritium per GW of power per year. The largest supply of tritium comes from Canadian fission reactors (CANDU) which operate with heavy water, which produce 130 g per year
Need tritium supply, with a tritium breeding ratio (TBR) > 1

## Slide 5: Fuel Cycle and Blanket Overview
Vacuum Pumping
Hydrogen Isotope Separation
Tritium Storage
Fueling System
Fuel Cleanup
Startup Inventory

## Slide 6: Fuel Cycle and Blanket Overview
Vacuum Pumping
Hydrogen Isotope Separation
Tritium Storage
Fueling System
Fuel Cleanup
+
fast neutrons
Startup Inventory
Tritium Breeding Blanket
Breeding Material
Multiplier(n, 2n)
Coolant

## Slide 7: Fuel Cycle and Blanket Overview
Vacuum Pumping
Hydrogen Isotope Separation
Tritium Storage
Fueling System
Fuel Cleanup
+
fast neutrons
Tritium Extraction
Heat Removal/
Power Extraction Cycle
Startup Inventory
Tritium Breeding Blanket
Breeding Material
Multiplier(n, 2n)
Coolant

## Slide 8: Fuel Cycle and Blanket Overview
Vacuum Pumping
Hydrogen Isotope Separation
Tritium Storage
Fueling System
Fuel Cleanup
+
fast neutrons
Tritium Extraction
Heat Removal/
Power Extraction Cycle
Startup Inventory
Tritium Breeding Blanket
Breeding Material
Multiplier(n, 2n)
Coolant

## Slide 9: Fuel Cycle and Blanket Overview
Vacuum Pumping
Hydrogen Isotope Separation
Tritium Storage
Fueling System
Fuel Cleanup
+
fast neutrons
Tritium Extraction
Heat Removal/
Power Extraction Cycle
Startup Inventory
Tritium Breeding Blanket
Breeding Material
Multiplier(n, 2n)
Coolant

## Slide 10: Fuel Cycle and Blanket Overview
Vacuum Pumping
Hydrogen Isotope Separation
Tritium Storage
Fueling System
Fuel Cleanup
+
fast neutrons
Tritium Extraction
Heat Removal/
Power Extraction Cycle
Startup Inventory
New Plants
Tritium Breeding Blanket
Breeding Material
Multiplier(n, 2n)
Coolant

## Slide 11: Fuel Cycle and Blanket Overview
Vacuum Pumping
Hydrogen Isotope Separation
Tritium Storage
Fueling System
Fuel Cleanup
+
fast neutrons
Tritium Extraction
Heat Removal/
Power Extraction Cycle
Exhaust/Water Detritiation Systems
Startup Inventory
New Plants
Waste Treatment
Waste Treatment
Tritium Breeding Blanket
Breeding Material
Multiplier(n, 2n)
Coolant

## Slide 12: Fuel Cycle and Blanket Overview
Vacuum Pumping
Hydrogen Isotope Separation
Tritium Storage
Fueling System
Fuel Cleanup
+
fast neutrons
Tritium Extraction
Heat Removal/
Power Extraction Cycle
Exhaust/Water Detritiation Systems
Startup Inventory
New Plants
Waste Treatment
Waste Treatment
Tritium Breeding Blanket
Breeding Material
Multiplier(n, 2n)
Coolant

## Slide 13: What is a blanket?
Functions
Tritium breeding
Heat generation/removal
Shielding
  magnets
  diagnostics
Structure

## Slide 14: What is a blanket?
Components
Structural Material
  Reduced activation materials
Tritium breeding material
  n + 6Li → 4He + T + 4.785 MeV
    Large cross section at thermal energies
    Exothermic: produces additional energy!
  n + 7Li → 4He + T + n’ - 2.5 MeV
    Produces tritium and a neutron
Multiplier material
  Elements that undergo (n,2n) reactions
  High (n,2n) cross section and low total absorption cross section
    Be and Pb are best
Coolant

## Slide 15: What is a blanket?
Components
Structural Material
  Reduced activation materials
Tritium breeding material
  n + 6Li → 4He + T + 4.785 MeV
    Large cross section at thermal energies
    Exothermic: produces additional energy!
  n + 7Li → 4He + T + n’ - 2.5 MeV
    Produces tritium and a neutron
Multiplier material
  Elements that undergo (n,2n) reactions
  High (n,2n) cross section and low total absorption cross section
    Be and Pb are best
Coolant

## Slide 16: Structural Materials
T. Muroga, 3/29/2022

## Slide 17: Activation of Structural Materials
D-T fusion creates waste
  Goal: Below Class C Low-Level Waste
Common alloying elements with long-lived radioisotopes
  Avoid Ni, Co, Mo, Nb, etc.
P. W. Humrickhouse, Fusion Science and Technology (2024, submitted)
7-12 MW at 1 s
Dominated by tungsten components, not blankets
Notes: When considering other elements in breeder, multiplier, or structural materials, neutron activation is a primary consideration

## Slide 18: Decay Heat
1
H
3
Li
4
Be
41
Nb
5
B
6
C
8
O
2
He
10
Ne
65
Tb
63
Eu
no
stable
isotopes
77
Ir
no
stable
isotopes
72
Hf
44
Ru
7
N
75
Re
76
Os
80
Hg
58
Ce
67
Ho
71
Lu
9
F
11
Na
12
Mg
13
Al
14
Si
15
P
16
S
17
Cl
18
Ar
19
K
20
Ca
21
Sc
22
Ti
23
V
24
Cr
31
Ga
32
Ge
33
As
35
Br
39
Y
40
Zr
42
Mo
47
Ag
48
Cd
49
In
52
Te
53
I
57
La
59
Pr
60
Nd
68
Er
69
Tm
70
Yb
74
W
79
Au
81
Tl
82
Pb
83
Bi
kW/kg
Top half of box:
at 10-5 years
Bottom half of box:
at 10-2 years
34
Se
51
Sb
25
Mn
26
Fe
27
Co
28
Ni
29
Cu
30
Zn
36
Kr
37
Rb
38
Sr
45
Rh
46
Pd
50
Sn
54
Xe
55
Cs
56
Ba
62
Sm
64
Gd
66
Dy
73
Ta
78
Pt
Based on C. B. A. Forty, et al., Handbook of Fusion Activation Data; Part 1. Elements Hydrogen to Zirconium, AEA FUS 180, May, 1992. Assumes 4.15 MW/m2 for 25 years
DH<10-4
10-4<DH<10-3
10-3<DH<10-2
10-2<DH<10-1
10-1<DH<100
100<DH<101
316 Stainless Steel

## Slide 19: Decay Heat
1
H
3
Li
4
Be
41
Nb
5
B
6
C
8
O
2
He
10
Ne
65
Tb
63
Eu
no
stable
isotopes
77
Ir
no
stable
isotopes
72
Hf
44
Ru
7
N
75
Re
76
Os
80
Hg
58
Ce
67
Ho
71
Lu
9
F
11
Na
12
Mg
13
Al
14
Si
15
P
16
S
17
Cl
18
Ar
19
K
20
Ca
21
Sc
22
Ti
23
V
24
Cr
31
Ga
32
Ge
33
As
35
Br
39
Y
40
Zr
42
Mo
47
Ag
48
Cd
49
In
52
Te
53
I
57
La
59
Pr
60
Nd
68
Er
69
Tm
70
Yb
74
W
79
Au
81
Tl
82
Pb
83
Bi
kW/kg
Top half of box:
at 10-5 years
Bottom half of box:
at 10-2 years
34
Se
51
Sb
25
Mn
26
Fe
27
Co
28
Ni
29
Cu
30
Zn
36
Kr
37
Rb
38
Sr
45
Rh
46
Pd
50
Sn
54
Xe
55
Cs
56
Ba
62
Sm
64
Gd
66
Dy
73
Ta
78
Pt
Based on C. B. A. Forty, et al., Handbook of Fusion Activation Data; Part 1. Elements Hydrogen to Zirconium, AEA FUS 180, May, 1992. Assumes 4.15 MW/m2 for 25 years
DH<10-4
10-4<DH<10-3
10-3<DH<10-2
10-2<DH<10-1
10-1<DH<100
100<DH<101
Inconel 718

## Slide 20: Decay Heat
RAFM Steel
1
H
3
Li
4
Be
41
Nb
5
B
6
C
8
O
2
He
10
Ne
65
Tb
63
Eu
no
stable
isotopes
77
Ir
no
stable
isotopes
72
Hf
44
Ru
7
N
75
Re
76
Os
80
Hg
58
Ce
67
Ho
71
Lu
9
F
11
Na
12
Mg
13
Al
14
Si
15
P
16
S
17
Cl
18
Ar
19
K
20
Ca
21
Sc
22
Ti
23
V
24
Cr
31
Ga
32
Ge
33
As
35
Br
39
Y
40
Zr
42
Mo
47
Ag
48
Cd
49
In
52
Te
53
I
57
La
59
Pr
60
Nd
68
Er
69
Tm
70
Yb
74
W
79
Au
81
Tl
82
Pb
83
Bi
kW/kg
Top half of box:
at 10-5 years
Bottom half of box:
at 10-2 years
34
Se
51
Sb
25
Mn
26
Fe
27
Co
28
Ni
29
Cu
30
Zn
36
Kr
37
Rb
38
Sr
45
Rh
46
Pd
50
Sn
54
Xe
55
Cs
56
Ba
62
Sm
64
Gd
66
Dy
73
Ta
78
Pt
Based on C. B. A. Forty, et al., Handbook of Fusion Activation Data; Part 1. Elements Hydrogen to Zirconium, AEA FUS 180, May, 1992. Assumes 4.15 MW/m2 for 25 years
DH<10-4
10-4<DH<10-3
10-3<DH<10-2
10-2<DH<10-1
10-1<DH<100
100<DH<101

## Slide 21: Alloy concentrations to meet Class C disposal
From: Piet, et al., “Initial Integration of Accident Safety, Waste Management, Recycling, Effluent, and Maintenance
Considerations for Low-Activation Materials”, Fusion Technology, Vol. 19, Jan. 1991, pp. 146-161.
Assumes 5 MW/m2 for 4 years; and E. T. Cheng, “Concentration Limits of Natural Elements
in Low Activation Materials”, presented at ICFRM-8, Sendai, Japan,October 1997
316 Stainless Steel

## Slide 22: Alloy concentrations to meet Class C disposal
From: Piet, et al., “Initial Integration of Accident Safety, Waste Management, Recycling, Effluent, and Maintenance
Considerations for Low-Activation Materials”, Fusion Technology, Vol. 19, Jan. 1991, pp. 146-161.
Assumes 5 MW/m2 for 4 years; and E. T. Cheng, “Concentration Limits of Natural Elements
in Low Activation Materials”, presented at ICFRM-8, Sendai, Japan,October 1997
Inconel 718

## Slide 23: Alloy concentrations to meet Class C disposal
From: Piet, et al., “Initial Integration of Accident Safety, Waste Management, Recycling, Effluent, and Maintenance
Considerations for Low-Activation Materials”, Fusion Technology, Vol. 19, Jan. 1991, pp. 146-161.
Assumes 5 MW/m2 for 4 years; and E. T. Cheng, “Concentration Limits of Natural Elements
in Low Activation Materials”, presented at ICFRM-8, Sendai, Japan,October 1997
RAFM Steel

## Slide 24: Activation of Structural Materials
Low-activation Materials
  Reduced-Activation Ferritic/Martensitic Steel – most mature fusion material ​
  Vanadium Alloys – need development​
  Silicon Carbide – need development​
= V alloy, Li2O
= RAFM steel, PbLi
= RAFM steel, Li4SiO4
= SiC composite, PbLi
= RAFM steel, PbLi
= SiC composite, Li4SiO4
M. Zucchetti, Fusion Engineering and Design 136 (2018) 1529-1533.
Notes: “No breeder can be developed without considering the combination with the coolant, neutron multiplier, and structural material - and this must be done in an integrated fashion, since the choice of each has an impact on the other”

## Slide 25: What is a blanket?
Components
Structural Material
  Reduced activation materials
Tritium breeding material
  n + 6Li → 4He + T + 4.785 MeV
    Large cross section at thermal energies
    Exothermic: produces additional energy
  n + 7Li → 4He + T + n’ - 2.5 MeV
    Produces tritium and a neutron
Multiplier material
  Elements that undergo (n,2n) reactions
  High (n,2n) cross section and low total absorption cross section
    Be and Pb are best
Coolant

## Slide 26: Tritium Breeding Materials
Liquid Metals
  Li
  PbLi
Solid Ceramics
  Li2TiO3, Li4SiO4, and many others possible
Molten Salts
  FLiBe (2LiF + BeF2)
  FLiNaBe (LiF + NaF + BeF2)
https://www.psfc.mit.edu/news/2022/turning-neutrons-into-fusion-fuel
S. Sharafat et al., Fusion Engineering and Design 109-111 (2016) 119-127 ​
High melt temperature ✕
 Highly Corrosive ✕
X. R. Wang et al., Fusion Science and Technology, vol. 67, no. 1, (2017) 193-219
Magnetohydrodynamic challenges
Relatively low melt temperature ✓
 More structure required
Lower TBR ✕

## Slide 27: Tritium Breeding Ratio for Different Materials
L. El-Guebaly, in “Fusion Energy and Power: Applications, Technologies and Challenges” (2015)
These go higher with multiplier addition
2m
solid breeder: helium is separate from coolant stream
Notes: Theoretical maximum TBR: plasma surrounded completely by thick (2m) blanket

## Slide 28: Lithium Enrichment
n + 6Li → 4He + T + 4.785 MeV
  Large cross section at thermal energies
  Exothermic: produces additional energy
  Li6 is only 7.5% of natural lithium
n + 7Li → 4He + T + n’ - 2.5 MeV
  Produces tritium and a neutron
How do you get desirable quantities of Li6?
 Enrichment!

## Slide 29: Methods of Breeding Tritium
Liquid Metal - Li
Good TBR; may not need 6Li enrichment
Low Tmelt = 180 °C
Traditionally paired with Vanadium alloy or RAFM steel structure
Very high chemical reactivity with H2O and air (safety issue)
High tritium solubility/inventory, different extraction techniques needed
Electrical insulators required for MFE
Liquid Metal - PbLi
Good TBR, but with 6Li enrichment
Low Tmelt = 235 °C
Traditionally paired with RAFM steel or SiC structure
Much lower chemical reactivity than pure Li
Low T/high T design options
Material compatibility at high T may require coatings
Electrical insulators required for MFE
Solid Ceramic
Good TBR requires Be multiplier addition, structure minimization
Traditionally paired with RAFM steel structure and He or H2O coolant
Better material compatibility than liquids
Simpler & more mature tritium extraction
Require replacement
Evolution under irradiation important
Molten Salt - FLiBe
Good TBR may require Be multiplier addition
High Tmelt = 460 °C
Corrosion a significant concern
Structural material solution unclear
Low electrical conductivity
High heat capacity
Low thermal conductivity
High viscosity

## Slide 30: What is a blanket?
Components
Structural Material
  Reduced activation materials
Tritium breeding material
  n + 6Li → 4He + T + 4.785 MeV
    Large cross section at thermal energies
    Exothermic: produces additional energy!
  n + 7Li → 4He + T + n’ - 2.5 MeV
    Produces tritium and a neutron
Multiplier material
  Elements that undergo (n,2n) reactions
  High (n,2n) cross section and low total absorption cross section
    Be and Pb are best
Coolant

## Slide 31: Multiplier Materials
TBR = 1  every fusion neutron produces tritium (unlikely)
  Need more neutrons!
F. Hernandez, Fusion Engineering and Design 137 (2018) 243-256.
M. Nakamichi, in Comprehensive Nuclear Materials 2nd ed (2020).
Be
Pb

## Slide 32: Lead, Beryllium and Beryllides
Lead
Must be in liquid form
Low radiation damage
Toxic
Impurities (Bismuth)
  Activation products
High (n, 2n) cross section
Relatively high total absorption cross section
Beryllium
Solid – high melt temperature
Toxic
Swelling due to irradiation
Tritium breeding; low tritium diffusivity (retention)
Highly exothermic reaction with air and water
Impurities (Uranium)
High (n, 2n) cross section
Low total absorption cross section
Beryllides (eg, Be12Ti)
Solid – high melt temperature
Toxic
Limits swelling
Limits chemical reactions
Tritium breeding; no retention
Large number of different beryllide compounds; some hard to work with
Impurities (Uranium)
Higher total absorption cross section than Be
Decreased atom density of Be

## Slide 33: What is a blanket?
Components
Structural Material
  Reduced activation materials
Tritium breeding material
  n + 6Li → 4He + T + 4.785 MeV
    Large cross section at thermal energies
    Exothermic: produces additional energy!
  n + 7Li → 4He + T + n’ - 2.5 MeV
    Produces tritium and a neutron
Multiplier material
  Elements that undergo (n,2n) reactions
  High (n,2n) cross section and low total absorption cross section
    Be and Pb are best
Coolant

## Slide 34: Blanket Cooling
Heat Removal
Remove heat from First Wall
  plasma
  neutrons
Remove heat due to volumetric heating
  heating in structural materials
  heat produced in exothermic reactions
  decay heat
Use for power conversation
First wall heat flux
Volumetric Heating

## Slide 35: Cooling mechanisms
Dual-Cooled
Uses a separate coolant and breeding material
Examples:
  Dual-Cooled Lead Lithium (DCLL)
  Helium-Cooled Ceramic Breeder (HCCB)
  Water-Cooled Ceramic Breeder (WCCB)
M. Abdou (2015). Blanket/first wall challenges and required R&D on the pathway to DEMO. Fusion Engineering and Design.
M. S. Tillack and S. Malang, "High performance PbLi blanket," 17th IEEE/NPSS Symposium Fusion Engineering

## Slide 36: Cooling mechanisms
Self-Cooled
Uses the same coolant and breeding material
Examples
  Self-Cooled Lead Lithium (SCLL)
  Self-Cooled Molten Salt
C. Wong, Fusion Eng. Des. 72 (2004) 245-275.
C. Wong, Fusion Sci. Technol. 47:3 (2005) 502-509

## Slide 37: Coolants and Their Challenges
Helium
(+) Inert
(-) Low thermal conductivity
(+) High specific heat capacity
(-) High pressure system
(-) Bad neutron shield
Water
(-) Steam reactions bad
(-) Tritiated water bad
(-) High pressure system
(+) High specific heat capacity
(+) Well-known pumping systems
(+) Neutron shield
Liquid Metal
(-) MHD pressure drop
(+) High thermal conductivity
(-) Corrosive
(+) Reasonable melt temperature
Reactivity
  (-) Lithium highly reactive with water and air
  (+) PbLi Less reactive
Specific Heat Capacity
  (-) Low specific heat capacity (PbLi)
  (+) High specific heat capacity (Li)
(+) Breeding Material
Molten Salt
(-) High viscous pressure drop
(-) Somewhat poor thermal conductivity
(-) Highly Corrosive
(-) High melt temperature
(+) High specific heat capacity
(+) Breeding material
(+) Neutron shield

## Slide 38: Conclusion
How can we use those neutrons?
Breeding tritium from lithium
  solid ceramic
  liquid metal
  molten salt
Make more neutrons with neutron multipliers
  Pb
  Be/Beryllides
Heating for power conversion
What challenges do those neutrons present?
Material activation and decay heat
  Requires careful material selection
Damage to solid structures
  need to shield sensitive components
Large heat load
  Careful selection of Breeding/Multiplier/Coolant material combinations

## Slide 39
Extra Slides

## Slide 40: Decay heat dependence on blanket concept
FNSF with PbLi replaced with other breeder/multiplier materials:
7-18 MW at 1 s
Dominated by 16N in FLiBe
46Sc (from Ti in multiplier) adds significantly in solid breeders
95Zr, 95Nb add significantly in Li2ZrO3 breeder
Blankets with high beryllium content lead to increased activation of FW and Divertor tungsten through multiplication, moderation of the neutron flux

## Slide 41: Lithium is the only solution
Lithium is the only element that can achieve a TBR > 1:
  n + 6Li → 4He + T + 4.785 MeV
    Large cross section at thermal energies
    Exothermic: produces additional energy!
  n + 7Li → 4He + T + n’ - 2.5 MeV
    Produces tritium and a neutron
A D-T fusion is essentially fueled with deuterium and lithium:
F. Hernandez, Fusion Engineering and Design 137 (2018) 243-256.

## Slide 42: Beryllium as a multiplier
Pb and Be are the only viable multipliers
Pure Be has a number of shortcomings as a multiplier material (aside from toxicity and resultant difficulty in manufacturing):
  High swelling under irradiation, especially at high temperature (> 600 °C)
  High tritium retention (40% at 600 °C)
    A small but significant (<1%) amount of tritium is bred in beryllium
    Diffusivity of tritium in beryllium metal is low (it would be a decent permeation barrier)
  High chemical reactivity…
F. A. Hernández, Fusion Engineering and Design 137 (2018) 243-256.
F. A. Hernández, Fusion Science and Technology 75 (2019) 352-364.

## Slide 43: Beryllium Oxidation
Beryllium reacts exothermically with steam and air; at high temperature the possibility for “runaway” reactions exists
For water-cooled ceramic breeder designs, this is a significant safety issue
So also for ITER (water cooling and beryllium PFCs)
Y. Someya, 2018 US-JA Workshop
Helium cooling avoids steam reactions, hydrogen generation
But should consider the event of air ingress, e.g. as a result of ex-vessel helium pipe break
R. A. Anderl, Journal of Nuclear Materials 258-263 (1998) 750-756.

## Slide 44: Beryllides
Need to inhibit oxidation led to a search for alternate materials with high beryllium content but better oxidation resistance
Focus on group 4-6 transition metal beryllide intermetallic compounds
  BeXM, where X=12 or 13; >92% beryllium
  Hard, brittle, high melt temperature (1500-1900 °C)
Early research performed by Brush Wellman (now Materion), funded by the air force, in search of new oxidation-resistant high temperature materials
None apparently found widespread application at that time, but high beryllium density, high temperature, oxidation resistant behavior makes them potentially attractive multipliers for ceramic breeder blankets

## Slide 45: Titanium Beryllide
Titanium beryllide, Be12Ti, is the first and most extensively studied beryllide for fusion applications
  Best neutron multiplier among the beryllides1
Irradiation to 19.5 dpa, 2740 appm He in HIDOBE-01 revealed much lower swelling and tritium retention compared to pure Be
M. Uchida, Fusion Engineering and Design 69 (2003) 499-503.
1C. Dorn, Fusion Engineering and Design 84 (2009) 319-322.
JMTR, 70 appm He, 0.5 dpa
A. V. Fedorov, Fusion Engineering and Design 102 (2016) 74-80.

## Slide 46: Titanium Beryllide Oxidation
Titanium beryllide (Be12Ti) amongst those characterized in early work by Brush Wellman1; not as extensively characterized as other beryllides, which outperformed it3
Complete oxidation:
TiO2 not observed in more recent air oxidation work; Be expected to reduce TiO22
Multiple studies suggest lower oxidation rates than pure Be; 6-20x lower in SCK-CEN studies4
1R. M. Paine, Corrosion 20 (1964) 307t-310t.
2P. Kurinsky, Fusion Engineering and Design 86 (2011) 2454-2457.
3C. Dorn, Fusion Engineering and Design 84 (2009) 319-322.
4F. Druyts, https://www.osti.gov/etdeweb/servlets/purl/20658771.
1
2
2
4