## Slide 1: Plasma-Material Interactions Hanna Schamis (PPPL) Introduction to Plasma and Fusion, June 18, 2024

## Slide 2: About me – how I got here
Grew up in Buenos Aires
University of Michigan (2016, BS Physics)
SULI at PPPL (x2!)
PPPL (2023 -- ??)
University of Illinois (2019, MS Nuclear, Plasma, and Radiological Engineering)
Penn State (PhD Nuclear Engineering)

## Slide 3: Disclaimer
This talk focuses on plasma material interactions (PMI) for fusion applications
Other areas where PMI is important:
  Semiconductor manufacturing
  Electric propulsion
  Solar wind/space weathering of asteroids
In this talk: “hydrogen” is short for “hydrogen isotopes” = H/D/T

## Slide 4: Plasmas affect materials
Wall
Heat, ion, and neutron fluxes
Melting
Cracking
Embrittlement
Transmutations
Erosion
Retention
Reflected particles
Sputtered atoms
Low or high recycling
Core impurities
Plasma
and materials affect plasmas

## Slide 5: Retention / Reflection / Recycling
describe different parts of the same process
C
C
C
C
C
C
C
C
C
C
C
C
C
C
Plasma
Wall
High Recycling fuel atoms cooling down and re-entering the plasma
Low Recycling fuel atoms retained in wall
+
Incoming fuel ion
0
Reflected fuel atom (lower energy)
0
Retained fuel atom

## Slide 6
1951: Spitzer recognized impurities from PMI could be a threat to plasma purity
1950 1960 1970 1980 1990 2000 2010 2020
[G. Federici, Nucl. Fusion, 2001; M. S. Parsons, Dissertation, 2023]
Wall conditioning
Plasma-facing materials

## Slide 7
1950 1960 1970 1980 1990 2000 2010 2020
[G. Federici, Nucl. Fusion, 2001; M. S. Parsons, Dissertation, 2023]
1951: Spitzer recognized impurities from PMI could be a threat to plasma purity
1950s: early stellarators had severely contaminated plasmas due to vacuum conditions.

## Slide 8
1960s: Early tokamaks contained large amounts of carbon, oxygen and metallic impurities, despite reduction efforts.
  Stainless steel vacuum vessel
  All-metal seals
  Baking
  Discharge cleaning
[G. Federici, Nucl. Fusion, 2001]
Wall conditioning
Removing impurities to improve plasma performance
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 9: Wall conditioning – Baking
Wall
Heat
To pumps

## Slide 10: Wall conditioning – Discharge Cleaning
Wall
Gas
(He, H)
Electrode 

## Slide 11
[G. Federici, Nucl. Fusion, 2001; P. Stangeby “The Plasma Boundary of Magnetic Fusion Devices,” 2000 ]
1960s: Early tokamaks contained large amounts of carbon, oxygen and metallic impurities, despite reduction efforts.
Late 1960s, early 1970s: Limiters are introduced
  Stainless steel
  Refractory metals (molybdenum, tungsten, titanium)
  Ceramics (boron carbide, alumina)
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 12
Mid-1970s: new divertors move contact surface further away from the core
  Scrape-off-layer (SOL): buffer zone between core and materials
[G. Federici, Nucl. Fusion, 2001; P. Stangeby “The Plasma Boundary of Magnetic Fusion Devices,” 2000 ]
X-point
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 13
Mid-1970s: new divertors move contact surface further away from the core
Late 1970s: Auxiliary heating (neutral beams) results in hotter plasmas
  Higher heat fluxes at the limiter, higher edge Te
  Princeton Large Torus had a tungsten limiter switched to graphite, reduced core radiation
[G. Federici, Nucl. Fusion, 2001; P. Stangeby “The Plasma Boundary of Magnetic Fusion Devices,” 2000; M. S. Parsons, Dissertation, 2023]
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 14
Early laboratory experiments of D  C
  High chemical sputtering
  Trapping of hydrogen in co-deposited layers
[G. Federici, Nucl. Fusion, 2001]
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 15: Sputtering processes
C
C
C
C
C
C
C
C
C
C
C
C
C
C
D
D
C
D
C
C
C
C
C
C
C
C
C
C
C
C
C
C
D
D
C
D
D
Physical Sputtering
Chemical Sputtering

## Slide 16: Material migration: re- and co-deposition
Redeposition
Co-Deposition
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
D
C
D
D
C
D
C
D
C

## Slide 17: Co- and re-deposition happens constantly in tokamaks and leads to thick mixed-material layers
From ASDEX upgrade:
Note: H/D/T can’t be detected in most surface analysis techniques
[A. Kallenbach J. of Nucl. Mater. 2011]

## Slide 18
Early laboratory experiments of D  C
First plasma-deposited coatings:
  Boronization
  Siliconization
  Carbonization
[G. Federici, Nucl. Fusion, 2001]
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 19: Wall conditioning – coatings
Wall
Gas
(He + B2D6)
Anode 

## Slide 20
Early laboratory experiments of D  C
First plasma-deposited coatings
Many tokamaks had graphite limiters/divertor plates
New tokamaks
  TEXTOR 1980 – 2013
  TFTR 1982 – 1997
  JET 1983 – 2023
  DIII-D 1986 – present
  Tore Supra 1988 – 2010 / WEST 2016 – present
[G. Federici, Nucl. Fusion, 2001]
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 21
TFTR ”Supershot”
  Q = 0.27
  Higher neutron rate
  Higher stored energy
  Higher energy confinement time
  Higher ion temperature
  Less carbon in core
[J.A. Snipes et al JNM 1992
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 22: Lithium as the plasma-facing material
NSTX Liquid Lithium Divertor and Lithium Evaporators (LITER)
H. W. Kugel et al., Fusion Engineering and Design, 2012

## Slide 23: Lithium as the plasma-facing material
NSTX-U Liquid Lithium Divertor and Lithium Evaporators (LITER)
Flowing liquid lithium concepts:
  Flowing liquid lithium (FLiLi) limiter
  Lithium Metal Infused Trenches (LiMIT)
[G. Z. Zuo PoP 2020; D. N. Ruzic NME 2017]

## Slide 24: Lithium as the plasma-facing material
NSTX-U Liquid Lithium Divertor and Lithium Evaporators (LITER)
Flowing liquid lithium concepts
Capillary porous systems
[P. Rindt, Nucl. Fusion 2019; C. López Pérez, Nucl. Mater. Energy 2023]

## Slide 25: Lithium as the plasma-facing material
NSTX-U Liquid Lithium Divertor and Lithium Evaporators (LITER)
Flowing liquid lithium concepts
Capillary porous systems
Lithium vapor box
[E. D. Emdee NF 2019]

## Slide 26: Lithium as the plasma-facing material
NSTX-U Liquid Lithium Divertor and Lithium Evaporators (LITER)
Flowing liquid lithium concepts
Capillary porous systems
Lithium vapor box
All-lithium walls: Lithium Tokamak eXperiment (LTX)
[D. P. Boyle, et al., PRL 2017]

## Slide 27
TFTR ”Supershot”
First ITER design
  Goal: Q > 10
  Divertor: CFC + W (later: just W)
  First wall: Be
[R. Aymar, et al. Plasma Phys. Control. Fusion 44 2002]
1950 1960 1970 1980 1990 2000 2010 2020

## Slide 28
2008: tungsten fuzz
1950 1960 1970 1980 1990 2000 2010 2020
[M. J. Baldwin, et al., Nuclear Fusion 48 (2008)]

## Slide 29
2008: tungsten fuzz
1950 1960 1970 1980 1990 2000 2010 2020
[D. Dasgupta, et al., Nuclear Fusion 59 (2019)]

## Slide 30
2011: JET ITER-like wall (ILW)
1950 1960 1970 1980 1990 2000 2010 2020
[L. Horton, et al., Fusion Engineering and Design, 2013]

## Slide 31
2011: JET ITER-like wall (ILW)
2015: DIII-D Metal Rings Campaign
1950 1960 1970 1980 1990 2000 2010 2020
[E. A. Unterberg, et al., Nuclear Materials and Energy, 2019]

## Slide 32
2011: JET ITER-like wall (ILW)
2015: DIII-D Metal Rings Campaign
2017: WEST operates with full W walls
1950 1960 1970 1980 1990 2000 2010 2020
[J. Bucalossi, et al., Nuclear Fusion, 2022]

## Slide 33
2011: JET ITER-like wall (ILW)
2015: DIII-D Metal Rings Campaign
2017: WEST operates with full W walls
2018: Impurity Powder Droppers
  Insert powders into plasma during plasma discharges
  Can be used with almost any powder (Li, Si, C)
  Installed on DIII-D, ASDEX-Upgrade, WEST, W7X, LHD, KSTAR and EAST
  Results: ELM suppression and mitigation, wall conditioning
1950 1960 1970 1980 1990 2000 2010 2020
[A. Nagy, et al., Rev. Sci. Instrum. 89 (2018)]

## Slide 34
2023: ITER updates its baseline
  Be first wall  W first wall
  Needs boronization
1950 1960 1970 1980 1990 2000 2010 2020
[H. Schamis, in preparation]

## Slide 35: Brief overview of other PMI topics: Divertor geometry
Snowflake divertor
  Additional null point
  4 strike points instead of 2
[D. D. Ryutov PoP 2015]

## Slide 36: Brief overview of other PMI topics: Divertor geometry
Snowflake divertor
  Additional null point
  4 strike points instead of 2
Long legged divertor
  Strike point further from X-point
[M.R.K. Wingram Nucl Fus 59 2019]

## Slide 37: Brief overview of other PMI topics: Detachment
Impurity seeding (e.g., Ne gas puffing) increases neutral pressure in SOL:
  Increases collisions and radiative losses
  Decreases heat flux
  Decreases Te
  Decreases ion impact energy
  Increases flux to the divertor plates
[R. Pitts, et al., Nuclear Materials and Energy 20 (2019)]

## Slide 38: Brief overview of other PMI topics: Novel materials
High-entropy alloys (HEAs)
  Example: W31 Ta34 Cr5 V27Hf3
[ O. El Atwani et al. Nature 2023,

## Slide 39: Brief overview of other PMI topics: Novel materials
High-entropy alloys (HEAs)
Dispersion-strengthened tungsten composites
  Transition metal carbide or oxide dispersoids
[T. Marchhart, et al., Sci. Rep. 2024]

## Slide 40: Brief overview of other PMI topics: Novel materials
High-entropy alloys (HEAs)
Dispersion-strengthened tungsten composites
Tungsten Fiber composites
  Tungsten fiber embedded in a tungsten matrix
[A. Karcher, et al., Nucl. Mater. Energy, 2021]

## Slide 41: Brief overview of other PMI topics: Novel materials
High-entropy alloys (HEAs)
Dispersion-strengthened tungsten composites
Tungsten Fiber composites
Tungsten and/or Tantalum cold spray
[R. Neu, et al., Nucl. Mater. Energy, 2023

## Slide 42: Semiconductors (aka the profitable plasma reactors)
Fine-tuned PMI processes are used for semiconductor manufacturing
  Film deposition (e.g., chemical or physical vapor deposition)
  Etching (chemical etching, or chemical or physical ion sputtering)
Substrate
Deposited Film
Photoresist
UV light
Mask
Etching

## Slide 43: Summary
PMI, like all research, builds upon decades of previous knowledge
Some PMI has been “accidental” – lithium
Themes recur – W limiters replaced with C in 1980s, and now many present-day devices use W divertors
No magic solution for PMI in fusion reactors
Lots of out-of-the-box ideas!

## Slide 44: What does PMI research look like? (or what it has looked like for me)
Small-scale laboratory experiments
Tokamak experiments
Computational PMI

## Slide 45: Useful References
General PMI
G. Federici et al 2001 Nucl. Fusion 41 1967 doi.org/10.1088/0029-5515/41/12/218

## Slide 46: Useful References
General PMI
G. Federici et al 2001 Nucl. Fusion 41 1967 doi.org/10.1088/0029-5515/41/12/218
  Covers every topic, look at the references within article
Tip: If article seems relevant, look at work citing it (“Cited by” on Google Scholar)

## Slide 47: Useful References
General PMI
G. Federici et al 2001 Nucl. Fusion 41 1967 doi.org/10.1088/0029-5515/41/12/218
M. A. Lieberman and A. J. Lichtenberg, “Principles of Plasma Discharges and Materials Processing” (2005)

## Slide 48: Useful References
General PMI
G. Federici et al 2001 Nucl. Fusion 41 1967 doi.org/10.1088/0029-5515/41/12/218
M. A. Lieberman and A. J. Lichtenberg, “Principles of Plasma Discharges and Materials Processing” (2005)
Scrape off Layers
P. Stangeby, “The Plasma Boundary of Magnetic Fusion Devices” (2000)
Wall Conditioning
J. Winter 1996 Plasma Phys. Control. Fusion 38 1503 doi.org/10.1088/0741-3335/38/9/001
Lithium:
R. Kaita 2019 Plasma Phys. Control. Fusion 61 113011 doi.org/10.1088/1361-6587/ab4156
Don’t overlook Theses and Dissertations! They often include long literature reviews on a topic